Silkwood 2

Type: Curtain – Can also be used as light upholstery

Composition: 100% wool

Yarn type: Staple

Binding: Sateen

Width: Approx. 140 cm, 55 inches

Weight: Approx. 520 g/lin.m, 17 oz/ly

Repeat: None

Foreign fibers may occur in light colours

Colour difference may occur

Cleaning: Please see the ISO symbols

Disinfection, see kvadrat.dk

More info: Care and maintenance kvadrat.dk

Due to the composition of natural fibers the curtain can hang longer depending on the height of the curtain, room temperature and humidity.

This might also happen for textiles woven in a very open construction or knitted textiles.

It is therefore recommended to avoid the use of weight, but an adjustment of the length might still be needed after a while. Also, a possibility to let the curtain touch the ground when hanging.

gBCED

! u

Abrasion

Approx. 20.000 Martindale rubs, EN ISO 12947

Pilling

Note 4-5, EN ISO 12945

Seam slippage

Seam parallel to warp: 2.3 mm parallel to weft: 4.1 mm

EN ISO 13 936-2 180 Newton

Lightfastness

Note 3-7 ISO 105-B02

Fastness to rubbing

Dry note 4-5 ISO 105-X12

Wet note 4-5 ISO 105-X12

Flame resistance

AS/NZS 1530.3

NFPA 701 with treatment  (AB 2998 compliant)

Only relevant when used as upholstery

BS 5852 Part 1

EN 1021-1/2

Free from added flame retardant chemicals as standard

Environmental benefits

Follow the EU Ecolabel dye restrictions incl. AZO dye

and heavy metal restrictions

REACH compliant

Californian Proposition 65 list compliant

LBC Red list compliant

Mono-material designed for circularity

Recyclable

Special recommendations

The curtain shall touch the floor, when hanging

Green building certificates

Greenguard Gold: Low chemical emission

Health Product Declaration (HPD): Declaring textile content and substance

Country of origin

United Kingdom

Warranty

2 years. See terms and conditions on kvadrat.dk

Kvadrat packaging and cardboard is recyclable. Cardboard material is FSC certified and / or contains recycled content.

For further information

kvadrat.dk